Radiation Lengths

Radiation length of mixture of elements is approximated by

1/X0 = wj/Xj

Where wj and Xj are the fraction by weight and the radiation length for the jth element.

SE4445

Density is taken from Dow Corning data sheet to be 2.36. The elemental content by weight I take from the tables used for the detailed pixel radiation length calculations which is at https://edms.cern.ch/file/890439/1/L1L2_1.1.xlsx

Si:  5.531%	Al:  45.222%	O: 43.351%	C: 4.717%	H: 1.1719%

Does this make sense? The density of aluminum oxide is about 4 g/cc. The radiation length from the Particle Data Tables for aluminum oxide is 27.94 g/cm2.

Carbon Foams

I assume the foam is pure carbon + air and ignore the air. The radiation length is then obtained just by scaling the densities compared to pure carbon. I take the carbon density to be 2.265 g/cc and the radiation length to be 42.7 g/cm2 and 18.8cm. I scale from the 18.8 cm hence the uniformity of 43 in the table.

Unloaded Epoxies

Here we attempt to address unloaded epoxies. There are various formulations for epoxies and I do not know the exact chemical formulation of the epoxies we plan to use.  Here are some radiation length examples I have found:

Density 	X0(g/cm2)	Source

1.19	41.6		 http://personalpages.to.infn.it/~tosello/EngMeet/ITSmat/SDD/Epotek-301-1.html

1.15	41.9		C18H20O3  (SCT barrel module assumption, I believe)

1.2	40.2		Araldite in SCT endcap note www.hep.man.ac.uk/atlas/radlen/RL-EC-Modules-v4.doc

42.6		Assuming H4C2N

Here is what is used for pixels for Araldite 420 A/B

The density of Hysol EA 9396 is 1.14 g/cc. The density of EX1515 neat resin is 1.17 g/cc. So in round numbers I take 42 g/cm2 for nominal structural, unloaded epoxy and for the epoxy(EX1515) component of the carbon fiber facings (see later).

Hysol 9396(70% by weight) and BN(30% by weight)

Essentially the same as unloaded epoxy.

CGL-7018

This is an aluminum-nitride gel adhesive with nominal cured density of about 2.5 g/cc(from vendor spec). The density of aluminum nitride is 3.26 g/cc and radiation length is about 27.5 g/cc. The chemical content of the filler is not known to me.  Assuming the filler is density 1.2 then the AlN fraction is about 0.63. This yields the values below.

EG7658

This is an AlN filled adhesive with a vendor stated density o f2.3 g/cc. Again assuming 1.2 for the “epoxy”, then the AlN fraction is about 0.47.

Facings

The density of, for example, K13D2U fiber is 2.15-2.2 g/cc. If one takes 2.2, then the radiation length is about 44 g/cm2, compared to the PDG value of 42.7 for graphite. Assuming the resin is 42 g/cm, then there is very little dependence on the fiber fraction.  Fiber fraction is usually quoted by volume so assuming 2.2 g/cc for the fiber and 1.17 g/cc for the resin, one gets the following densities for different fiber volume fractions

70%	1.89 g/cc

65	1.84

60	1.79

55	1.74

50	1.69

45	1.63

40	1.58

So for 70% fiber fraction

And for 40% fiber fraction

| Element | X0(g/cm^2) | Fraction |
| --- | --- | --- |
| C | 44 | 0.556 |
| Resin | 42 | 0.444 |
| Density | 1.58 |  |
| 1/X0 | 0.02320779 |  |
| X0 | 43.09 | g/cm^2 |
| X0 | 27.27 | cm |

Here is what is used for pixels for YSH-80/EX1515(I assume density of 1.7, not well known but g/cm2 does not depend on this). I do not know the origin of this calculation.

I talk 43 g/cm2 for facings, with the understanding that this may be good to about 5%.

Honeycomb

The radiation length in g/cm2 should be about the same (43 g/cm2) as the facings since the resin is the same although the fiber is different(M46J). The vendor density of the honeycomb is stated to be 3.5 lb/cu ft. This is 0.0562 g/cc which gives a radiation length of 765 cm.

Stainless Steel

304 as below

Carbon-Carbon

The density of the carbon-carbon may vary. A table is given below for different densities assuming  that the radiation length for density 2.265 g/cc is 18.8 cm.

Diamond

Silicon

Take the PDG value for silicon of density 2.33, 21.82 g/cm2 and 9.36 cm.

Solder

Take eutectic 63% Sn and 37% Pb.  Yields 7.72 g/cm2. Density is 8.8 g/cc. So radiation length is 0.88 cm.